Fibrinogen PEGylation

Materials

Fibrinogen (Type I-S from bovine plasma, 65%, 166kDa, Sigma F4753)

Linear Poly(ethylene glycol) Diacrylate (PEGDA)

Tris(2-carboxyethyl)phosphine hydrochloride (TCEP) (Sigma C4706)

PBS + 8M Urea pH 7.4

Dialysis bag (MWCO 12,000-14,000)

Procedure

Product Reaction

- Clean all dishes to be used with acetone to clear organics.

- Warm up Fibrinogen to room temperature before opening!

- Weigh 0.25g Fibrinogen (net weight! in case of 65%, weigh 0.385g) and place in a 250mL Erlenmeyer flask.

- Dissolve Fibrinogen in 8M Urea in PBS pH 7.4 to final concentration of 7mg/ml (35.7mL).  Add stir bar and stir slowly (avoid foaming).

- Add 2-fold excess of TCEP (excess to fibrinogen cysteines, 62) (26 mg) and continue to stir.

- Adjust pH of solution to pH=8.

- Weigh 4-fold excess PEGDA (10kDa, 1.82g) in a centrifuge tube.

- Dissolve PEGDA in 8M Urea in PBS to final concentraion of 280mg/ml (6.5 mL), vortex, and centrifuge for 1-2min at 2500RPM to clear.

- Once clear (may take more than one centrifuge), add PEGDA solution to flask slowly.

- Cover the flask in foil completely, and allow to react at RT for 3hrs.

Precipitation

- After reaction, transfer solution to 500mL flask and dilute by 2 with 8M Urea in PBS pH 7.4 (42mL) – continue to stir.

- Add 4 volumes of acetone (328mL) and stir vigorously.  Transfer quickly to separation funnel.

- PEGylated Fibrinogen should precipitate almost immediately and migrate toward the bottom of the funnel.  Allow product to gather at the bottom completely (15-20min).  Transfer precipitate to 50mL centrifuge tube.

Purification

- Centrifuge for 2-3min at 2500RPM to separate product from acetone – should get about 5mL of product.

- Aspirate acetone supernatant and dissolve precipitate in 8-9mL of 8M Urea in PBS pH 7.4.

- Centrifuge for 1-2min at 2500RPM to remove air bubbles – solution should be clear.

- Transfer solution to dialysis bag, removing as many air bubbles as you can, and secure with clips.

- Dialyze product against 1L PBS over 24hrs (change 3X) under complete foil wrap at 4oC.

- Remove product solution from dialysis bag and aliquot into sterile microcentrifuge tubes.  Store in dark at -20oC.

Characterization

- First, test ability of solution to form gels by adding radical and exposing to UV light.  Also, check gels under phase microscope to ensure homogeneous polymerization.

- Perform BCA analysis to obtain protein (fibrinogen) concentration (usually 4-7mg/ml)

- Lyophilize exact volumes of product in tared microcentrifuge tubes to determine total product concentration.  Subtract fibrinogen concentration to obtain PEGylation efficiency (10-20mg/ml).  Be sure to substract PBS salts from product weight (9.88mg/ml).